## Slide 1: Interference Fit Fastener – Working Group
Robert Pilarczyk rtpilarczyk@hill-engineering.com
Working Group on Engineered Residual Stress Implementation

## Slide 2: FE model – fastener installation
Abaqus 3D model, quarter-symmetric
Boundary conditions below
Frictionless contact between pin and bore
Incrementally push the oversized pin into the hole
Hole diameter = 0.25”
Min pin diameter = 0.25”
Max pin diameter set to give desired interference
Transition chamfer length constant at 0.025”
Results in different chamfer angles for different interference
Also ran the models with a more aggressive chamfer
12.7 deg constant angle at transition
Push pin in along this direction
y symmetry
x symmetry
x,z fixed on back surf.
x fixed on this surf.
Quarter-symmetric pin
Chamfer 0.025” length
Bore surface

## Slide 3: 0.3% interference
Step 1 – push pin in
Step 2 – remove pin

## Slide 4: FE model results – 0.3% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 5: FE model results – 0.3% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 6: FE model results – 0.3% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial

## Slide 7: FE model results – 0.3% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial

## Slide 8: 0.6% interference
Step 1 – push pin in
Step 2 – remove pin

## Slide 9: FE model results – 0.6% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 10: FE model results – 0.6% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 11: FE model results – 0.6% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial
Bore
Hoop stress
Radial stress

## Slide 12: FE model results – 0.6% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress
Bore

## Slide 13: 1.2% interference
Step 1 – push pin in
Step 2 – remove pin

## Slide 14: FE model results – 1.2% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 15: FE model results – 1.2% interf.
Step 1
Pin installed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 16: FE model results – 1.2% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 17: FE model results – 1.2% interf.
Step 2
Pin removed
Stress
Strain
Hoop
Radial
Hoop stress
Radial stress

## Slide 18: Contour plot comparisons

## Slide 19: 0.3% interference – hoop stress
Pin installed
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
-20 to 20 ksi scale
Pin installed
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
-30 to 50 ksi scale

## Slide 20: 1.2% interference – hoop stress
Pin installed
Pin removed
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
-70 to 40 ksi scale
-90 to 20 ksi scale

## Slide 21: 1.2% interference – radial stress
Pin installed
Pin removed
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
More aggressive
12.7 deg chamfer
Less aggressive
< 3 deg chamfer over 0.025”
-70 to 20 ksi scale
-30 to 10 ksi scale

## Slide 22: Comparisons

## Slide 23: Comparison – 0.3% interference

## Slide 24: Comparison – 0.3% interference

## Slide 25: Comparison – 1.2% interference

## Slide 26: Comparison – 1.2% interference

## Slide 27: Comparison – 1.2% interference, no remote load
Models that push the pin into the hole show compressive hoop stress near the bore
Similar results found previously (HOLSIP reference by FTI)
~ 1.8% interference
More aggressive pin transition
Less aggressive pin transition
Another model with pin pushed in