## Slide 1: Interference Fit Fastener – Working Group
Robert Pilarczyk rtpilarczyk@hill-engineering.com
Working Group on Engineered Residual Stress Implementation

## Slide 2: Agenda
Group 1 – Open Hole Results
  Summary of submissions
  Data review and discussion
Fastener Installation
  Process differences and discussion

## Slide 3: Group 1 – Open Hole Results
Summary of submissions

## Slide 4: Group 1 – Open Hole Results
Summary of submissions

## Slide 5: Group 1 – Open Hole Results
Data review

## Slide 6: Group 1 – Open Hole Results
Data review

## Slide 7: Group 1 – Open Hole Results
Data review

## Slide 8: Group 1 – Open Hole Results
Data review

## Slide 9: Group 1 – Open Hole Results
Data review

## Slide 10: Group 1 – Open Hole Results
Data review

## Slide 11: Fastener Geometry and Installation
Fasteners have a transition region
  From threaded portion to straight shank
    Chamfer/fillet
  Depending on modeling approach, this geometric feature could be important
  Specifications don’t always detail this geometry in specifications
    ¼” Hi-Loks initial “rough” measurements indicate transition length of 0.025”
      In the process of measuring actual fasteners
Notice a small step in diameter here
http://www.jet-tek.com/hi-lok-pins/hl18.pdf

## Slide 12: Fastener Geometry and Installation
Additional references

## Slide 13: Fastener Geometry and Installation
FE modeling shows a significant influence of the chamfer geometry
  3D model, nonlinear elastic-plastic
  Fastener is incrementally pushed into the hole
    Solution for equilibrium for each incremental step
  More aggressive chamfer leads to higher levels of plasticity near the fastener entry side
  Longer, more gentle chamfer leads to lower levels of plasticity and more uniform results through the thickness
  Equivalent plastic strain comparison below
Equivalent plastic strain (PEEQ)
0.025” chamfer (more gradual transition)
Bore
Hole edge
0.010” chamfer (more abrupt transition)
Fastener entrance
Fastener exit
Installation direction

## Slide 14: Fastener Geometry and Installation
FE modeling shows a significant influence of the chamfer geometry
  Influence of chamfer geometry on hoop stress field below
  More abrupt transition leads to more variation through the thickness near the bore
  More gradual transition leads to a stress field more uniform through the thickness
    Similar to what would be obtained with a simplified model expanding the entire bore surface at once
Hoop stress (fastener installed)
0.025” chamfer (more gradual transition)
0.010” chamfer (more abrupt transition)

## Slide 15: Fastener Geometry and Installation
Fastener installation
  Varies based on fastener type
    Hi-Loks typically driven or drawn into the hole with rivet gun or screw-driven process
  What fastener system/s should we focus on?
    Threaded fasteners
    Solid rivets
    Tapered fasteners
    Others may not have reliable interference levels